## PLYWOOD SPECIFICATIONS

Issued October 14, 1996

### GENERAL USE PLYWOOD WITH HARDWOOD FACE VENEER

### 1.THE SCOPE OF SPECIFICATION

#### The specification covers general use plywood with hardwood face veneer.

##### The specification does not apply to customized plywood or film faced plywood.

##### Obligatory requirements to the plywood quality are covered in 3.3, 4.2, 5.1, 5.8.

### 2. CLASSIFICATION AND SIZES

### 2.1. The classification of plywood is based on the following criteria: the quality of the face veneer, water resistance degree of glue bond, the degree of face veneer treatment.

#### 2.1.1. Based on the quality of the face veneer plywood is subdivided into grades: E (elite), I, II, III, IV. Descriptions of the face grades of the plywood are specified in Supplement A.

#### 2.1.2. Based on water resistance degree of glue bond plywood is subdivided into the following:

### FSF - waterproof plywood

### FK - water resistant plywood

#### 2.1.3. Based on the degree of face veneer treatment plywood is subdivided into:

### Non-sanded (NS)

### Sanded on one side (S1)

### Sanded on two sides (S2)

#### 2.2. SIZES

#### 2.2.1. The sizes of plywood sheets and the number of plies in a sheet should correspond to those stated in Tables 1, 2.

### TABLE 1.

### (mm)

| Sheet Length (Width) | Maximum Deviation |
| --- | --- |
| 1200,1220,1250 | +/- 3.0 |
| 1500,1525,1800,1830 | +/- 4.0 |
| 2100,2135,2440,2500 | +/- 4.0 |
| 2700,2745,3050,3600,3660 | +/- 6.0 |

### Note: Plywood in other sizes can be produced if stipulated by a contract.

### TABLE 2.

### (mm)

| Nominal Plywood Thicknessd | Minimum Number of Plies | Sanded Plywood Maximum Deviation | Sanded Plywood Different Thickness | Non-sanded Maximum Deviation | Non-sanded Different Thickness |
| --- | --- | --- | --- | --- | --- |
| 3 mm | 3 | +0.3/-0.4 |  | +0.4/-0.3 |  |
| 4 | 3 | +0.3/-0.5 |  | +0.8/-0.4 |  |
| 6 | 5 | +0.4/-0.5 |  | +0.9/-0.4 | 1.0 |
| 9 | 7 | +0.4/-0.6 |  | +1.0/-0.5 |  |
| 12 | 9 | +0.5/-0.7 | 0.6 | +1.1/-0.6 |  |
| 15 | 11 | +0.6/-0.8 |  | +1.2/-0.7 |  |
| 18 | 13 | +0.7/-0.9 |  | +1.3/-0.8 |  |
| 21 | 15 | +0.8/-1.0 |  | +1.4/-0.9 | 1.5 |
| 24 | 17 | +0.9/-1.1 |  | +1.5/-1.0 |  |
| 27 | 19 | +1.0/-1.2 | 1.0 | +1.6/-1.1 | 2.0 |
| 30 | 21 | +1.1/-1.3 |  | +1.7/-1.2 |  |

### Note: Plywood of a different thickness and with a different number of plies in a sheet can be produced if stipulated by a contract. Then the deviations are calculated by the following formulae:

#### for sanded plywood:

### +(0,2+0,03 Sp), (1)

### -(0,4+0,03 Sp); (2)

### for non-sanded plywood:

### +(0,8+0,03 Sp), (3)

### -(0,3+0,03 Sp), (4)

### where Sp - nominal plywood thickness

#### 2.2.2. Plywood sheets should be cut at a square angle. Deviation must not exceed 2 mm per 1 lineal meter.

#### 2.2.3. Plywood marking should include:

### product name,

### core and face plies species,

### glue bond (based on water resistance),

### combination of face veneer species,

### formaldehyde emission class,

### type of surface treatment,

### sizes,

### reference to the Specification (GOST 3916.1-96)

#### Here is an example of marking birch plywood with core plies made of birch veneer, water resistant, combination of face veneer grades I/III, emission class E1, sanded on 2 sides, 2440 mm long, 1525 mm wide, 9 mm thick.

#### Birch plywood/birch, FK, I/III, E1, S2, 2440*1220*9 GOST 3916.1-96

### 3. TECHNICAL REQUIREMENTS

#### 3.1.1. Such wood species as birch, alder, maple, elm, beech, asp, poplar and lime are used to produce plywood face veneers. The same species as well as pine, spruce, fir, larch and cedar are used for core plies production. Plywood is considered to be produced of the species used for making its face veneers. Plywood can be made of one or more wood species, therefore it is divided into "homogeneous" and "combined".

#### If the number of veneer plies is even, the direction of fibers of the two middle plies must be parallel. Veneers, located symmetrically in the plywood, must be of the same species and thickness. The thickness of the veneer used for face plies must not exceed 3.5 mm, for core plies - 4 mm

#### 3.1.2. In face plies wood flaws and manufacturing defects exceeding the limits stated in Table 3 are not allowed.

#### 3.1.3. In core plies wood flaws and manufacturing defects are allowed if they do not influence the quality and the size of the plywood, stated in the Specification.

#### 3.1.4. Table 3 states the maximum number of permitted flaws and manufacturing defects on the plywood surface.

### TABLE 3. PLYWOOD DEFECTS DESCRIPTION AND LIMITATIONS

| Wood flaws, manufacturing defects underGOST 30427 | E grade plywood face veneers | I grade plywood face veneers | II grade plywood face veneers | II grade plywood face veneers | IV grade plywood face veneers |
| --- | --- | --- | --- | --- | --- |
| 1.Pin knots | Not allowed | Max 3 per M2 allowed | Allowed |
| 2.Sound lights and/or dark knots | Not allowed | Max 5 per m2, 15mm diam. cracks max 0,5mm wide | Max 10 per m2, 25mm diam. cracks max 1mm wide | Cracks max 1,5mm wide |
| 3.Loose knots or with/without knot holes, worn holes in cluster or scattered | Not allowed | Up to 3, max 6mm diam. | Up to 6, max 6mm diam. | Unlimited, max 40 diam. |
| 4.Small cracks/splits | Not allowed | Up to 2 per 1m2, max 200mm long | Allowed |
| 5.Wide cracks/splits | Not allowed | Up to 2 per 1m2 filled with putty, max 200mm long | Allowed |
| 6.Light mold | Not allowed | Allowed |
| 7.Dark mold | Not allowed | See item 2 of the Table | Allowed |
| 8.Deviation in wood structure | Very insignificant,incidental disposition | Allowed |
| 9.Light color variation | Not allowed | Allowed, no more than 5% of the sheet surface | Allowed |
| 10.Strong color variation | Not allowed | Allowed |
| 11.Decay | Not allowed |
| 12.Pinholes | Not allowed | See item 3 of the Table |
| 13.Face veneer overlap | Not allowed | Max 1 overlap 100 mm wide per 1 m2 | Max 2 overlaps 200 mm wide per 1m2 | Allowed |
| 14.Lack of veneer, sheet edge defects due to sanding or squaring | Not allowed | Max 2 mm wide | Max 4 mm wide | Max 5 mm wide |
| 15.Glue band | Not allowed | Allowed in non-sanded plywood |
| 16.Glue exudation | Not allowed | Allowed no more than 2% of sheet surface | Allowed no more than 5% of sheet surface | Allowed |
| 17.Scratches | Not allowed | Allowed |
| 18.Hollows or imprints | Not allowed | Allowed if depth/height is in range of thickness deviation | Allowed |
| 19.Fiber lift-up | Not allowed | Max on 5% of sheet surface | Max on 15% of sheet surface | Allowed |
| 20.Overpolishing | Not allowed | Allowed |
| 21.Crook | Does not apply to plywood up to 6.5mm thick. If over 6.5 mm thick then allowed with sag of no more than 15mm over 1M sheet's diagonal length |
| 22.Metal inclusions | Not allowed | Color metal staples |
| 23.Joint gaps | Not allowed | Max 1 piece 1 mm wide on 1 m2 of sheet | Max 2 piece 1 mm wide on 1 m2 of sheet | Allowed |
| 24.Decrepitation bubbles, etc | Not allowed |
| 25.Waviness(for sanded plywood), fuzziness | Not allowed | Allowed |
| 26.Scuffleness | Scuffleness parameter(Rm) under GOST 7016 is max 100 micron for sanded plywood and 200 micron for non-sanded plywood |
| 27.Wooden plugs | Not allowed | Max 8 pieces when plugging per 1m2 of sheet | Allowed |
| 28.Overlapped plugs | Not allowed | Max 2 pieces per 1m2 of panel | Allowed |

### Note:

### Norm of manufacturing defects "lack of veneer" refers both to outer and core plies.

### Wood and manufacturing defects which are not mentioned in Table 3 are not allowed.

### TABLE 4

### (pieces)

| Face Veneer Grade | Maximum of permitted wood flaws and manufacturing defects |
| --- | --- |
| E | No visible defects |
| I | 3 |
| II | 6 |
| III | 9 |
| IV | Number of wood flaws and manufacturing defects is unlimited. Sizes are limited according to items 3,5,11,12,14,24 of Table 3 |

### 3.1.6. In plywood less than 1525 mm wide E grade face ply may be made up of 2 pieces of veneer with a joint in the middle of the sheet. In plywood 1525 mm wide E grade face ply may be made up of 3 veneer pieces similar in width. Grade I and II face plies are allowed to be made up of unlimited number of veneer pieces.

#### Veneer joints for grades E, II, III should be parallel to sheet edges, veneer pieces should match in color

#### 3.1.7. Veneer plugs should be even with the surface, hold strongly and match face veneer in color and fiber direction. For grades I and II plugs should match the color of the wood.

#### Putties should match the color of wood, provide easy gluing, retain their color during plywood treatment and not crack when bending.

#### 3.2 Physical and mathematical parameters of plywood are stated in Table 5.

### TABLE 5

| Parametr | Thickness(mm) | Glue bond | Birch | Alder Beech | Pine Larch Fir Silverfir Cedar | Lime Asp Poplar |
| --- | --- | --- | --- | --- | --- | --- |
| Moisure content | 3-30 | FSF FK | 5-10 | 5-10 | 5-10 | 5-10 |
| Shear strenght (MPa) min |
| after boiling in water for 1 hour | 3-30 | FSF | 1,5 | 1,2 | 1,0 | 0,6 |
| after soaking in water for 24 hours |  | FK | 1,5 | 1,0 | 1,0 | 0,6 |
| Minimum static bending strength of fibres (MPa) | 9-30 | FSF | 60 | 50 | 40 | 30 |
|  |  | FK | 55,0 | 45,0 | 35,0 | 25,0 |
| Minimum tensile strength along fibers (MPa) | 3-6,5 | FSF | 40,0 | 40,0 | 40,0 | 40,0 |
|  |  | FK | 30,0 | 30,0 | 30,0 | 30,0 |

### Note: Birch plywood with shear strength along glue line of 1.2. Mpa is permitted if stipulated by a contract